## Slide 1
Years 2024 – 2025
Realisation and installation of electrodes to study the electrical properties of graphene
CROZAT Ilan
4A GPSE

## Slide 2
Introduction : A world in crisis
Polytech Orleans
Ilan CROZAT
2024 - 2025
Increase of the pollution :
Increase of the world population
Overcunsumption
Development of new and more calorific energy (fossil fuel)
In EU : 200 000 premature death in 2024 due of fine particles, and threatens the biodiversity of forest :
The aim ? Reducing pollution
2

## Slide 3
Project purpose : a captor made with graphene
Polytech Orleans
Ilan CROZAT
2024 - 2025
The global project : Develop a pollution sensor
3
Pollution sensor
Growing demand from companies and the public sector
We want : more precise and more reliable
Graphene structure

## Slide 4
Our project
Polytech Orleans
Ilan CROZAT
2024 - 2025
4
Our project
Take part of the global project
Studying our graphene properties
Research to made products with different conditions and materials from those of current market sensors

## Slide 5
Summary
Polytech Orleans
Ilan CROZAT
2024 - 2025
5
Summary
I . 1 : Octopus diagram
I . 2 : Use-case diagram
II . 1 : Peek substrat
II . 2 : Graphene and electrodes deposit
II . 3 : Goals and difficulties
III . 1 : Graphite thickness
III . 2 : Mask, design and charaterization
III . 3 : Process flow
IV . 1 : Process-flow application
IV . 2 : Carbon observation with the VHX
IV . 3 : Resist gap
IV . 4 : Observation of the deposed metal
V . 1 : Final charaterization
I . Fonctional bloks
II . Project purpose
III . Conception
IV . Fabrication and observation
V . Charaterization
Conclusion
Bibliography

## Slide 6
I . 1 : Octopus diagram
Polytech Orleans
Ilan CROZAT
2024 - 2025
6

## Slide 7
I . 2 : Use-case diagram
Polytech Orleans
Ilan CROZAT
2024 - 2025
7

## Slide 8
II . 1 : Peek substrat
Polytech Orleans
Ilan CROZAT
2024 - 2025
8
w = 1,7 cm
l = 2,4 cm
Peek substrat
Peek diagram

## Slide 9
II . 2 : Graphene and electrodes deposit
Polytech Orleans
Ilan CROZAT
2024 - 2025
9
Peek substrat with graphene, and electrodes

## Slide 10
- Designing a process-flow of electrodes on a Peek substrate
- Electrodes fabrication on a carbon-containing substrate
- Graphene charaterization and identification
II . 3 : Goals and difficulties
Polytech Orleans
Ilan CROZAT
2024 - 2025
10
Goals
Dificulties
Conception on Peek : Lack of data, non-adapted material, rough surface…
- Mechanical / Thermal propriety
- Carbon fabrication using laser pulses : modular, precise
Designing the electrodes without any dimension for carbon surfaces

## Slide 11
III . 1 : Graphite thickness
Polytech Orleans
Ilan CROZAT
2024 - 2025
11
Thickness :
Resistivity charaterization of the graphene
Carbon thickness can be determined

## Slide 12
III . 2 : Mask, design and charaterization
Polytech Orleans
Ilan CROZAT
2024 - 2025
12
Inital idea of the mask design
Final version of 6 diffrent mask
Mask :
- Use to give the design of the electrodes
- A part lets the UV rays through, the other is opaque
Pattern :
Centered to assure balance during UV insolation
One huge electrode in a side, several in the other side
6 version : one has been used

## Slide 13
III . 2 : Mask, design and charaterization
Polytech Orleans
Ilan CROZAT
2024 - 2025
13
Diagram of the substrat with electrodes
- Designing several « ways » to charaterize different carbon surfaces
Design :
Lowest carbon density
Highest carbon density
- One huge electrode to make the resistivity measurement report

## Slide 14
III . 3 : Process flow
Polytech Orleans
Ilan CROZAT
2024 - 2025
14
1
2
3
4
5
6
7
8
Peek substrat with graphene
A layer of LOR20B and S1813 (positive resit) deposition, and spreading on the substrat.
Mask applying + UV irradiation.
Removal of S1813 weakened by UV rays.
LOR20B dug by developer product
Metal deposit with two layers :
Lift-off process : removal of all the remaining resist
Final product
SVC-14
MF-319
Diagram animation of T-Pop process
- Designing a process-flow of electrodes on a Peek substrate

## Slide 15
Polytech Orleans
Ilan CROZAT
2024 - 2025
15
IV . 1 : Process-flow application
Before metal deposit
After metal deposit
LOR20B and S1813
After the photolithography
Final product
- Electrodes fabrication on a carbon-containing substrate
T-Pop process diagram

## Slide 16
Polytech Orleans
Ilan CROZAT
2024 - 2025
16
IV . 2 : Carbon observation with the VHX
Peek substrat with carbon surface

## Slide 17
Polytech Orleans
Ilan CROZAT
2024 - 2025
17
IV . 3 : Resist gap
We can see it on digital microscope
Means that our T-Pop process worked
Resist gap :
Resist gap on VHX

## Slide 18
Polytech Orleans
Ilan CROZAT
2024 - 2025
18
IV . 4 : Observation of the deposed metal
The metal as been deposited well
Impossible to measure thickness : < um ?
After metal deposit :

## Slide 19
V . 1 : Final charaterization
Polytech Orleans
Ilan CROZAT
2024 - 2025
19
No conductivity found
- Non-homogenous carbon ?
- Carbon removed during the fabrication process ?
Characterization :
Enhance the process-flow to reduce possible damage
Set up a program with the double needle
Be totally sure about the conductivity of the carbon first
Enhance ideas :
Two needles charaterization
Multimeter
- Graphene charaterization and identification

## Slide 20
Conlusion
Polytech Orleans
Ilan CROZAT
2024 - 2025
20
- Designing a process-flow of electrodes on a Peek substrate
- Electrodes fabrication on a carbon-containing substrate
- Graphene charaterization and identification
Goals
Prospects
Improving the process-flow
Enhance the conception and the design
Using different materials and equipment (metal, rays insolation…)
Skills
Level 2 :
Designing a technological microfabrication process flow
Project follow-up
Level 1 :
Perform micro-fabrication steps in a clean room
Writing a progress report
Personnal
Interesting and instructive project
Acquiring and strengthening microfabrication skills
Project in line with my 4th year internship

## Slide 21
Bibliography
Polytech Orleans
Ilan CROZAT
2024 - 2025
21
Bibliography
Premature deaths due to pollution: - INED
- https://www.ined.fr/fichier/s_rubrique/19627/extraits_urbanisation_monde.fr.pdf
Urbanization of the world: European Environment Agency (EEA) .
https://www.eea.europa.eu/fr/highlights/le-nombre-de-deces-prematures
Combining printed electronics and graphene sensors to accelerate PFD detection
https://www.actu-environnement.com
Lithography techniques: MOOC
lms.fun-mooc.fr

## Slide 22
Polytech Orleans
Ilan CROZAT
2024 - 2025
19
The End
Thanks for listening

## Slide 23
Pollution sensor with graphene
Executive process
Development of electrode implementation process
Characterization of the product
- Marketing to bring income on research
Market analysis
- Target audience : Biomedical, electronic…
High demand on new material, technology
Business model
Direct incomes :
Licence on the new technology (investment)
Partnership with the research center
Cost structure :
R&D structure
Equipment, area of research
Financial strategy
- Funding source : State, R&D investor…
Return on investment (long term)
Development plan
R&D phase, design creation, theory learning
Characterization phase, testing
Industrialisation
Commercialization
Annexe

## Slide 24
Annexe

## Slide 25
Annexe